## Slide 1: Toward a sustainable future: Investigating the nanocrystalline structure and properties of C-(N)-A-S-H gels.
Theodosios Dimitrasopoulos

## Slide 2: Overview
Introduction & background;
Research question;
Materials and Methods;
Findings;
Summary and conclusion; Further work.

## Slide 3: Introduction
1 ton Ordinary Portland Cement (OPC) | 1 ton CO2
OPC content reduction in concrete
Supplementary Cementitious Materials (SCM) | “additives”
Alkali-activated materials (AAM)

## Slide 4: Introduction
Calcium Silicate Hydrate (CSH)
Calcium Alumino-silicate Hydrate (CASH)
1. Schematic representation of CSH gel
2. Schematic representation of CASH gel

## Slide 5: Research question
“What is the nanocrystalline structure and properties of C-(N)-A-S-H gels as compared to C-S-H? Are alkali-activated materials a viable solution to the substitution of OPC in concrete?”

## Slide 6: Materials & Methods
X-Ray Powder Diffraction & Scattering (Bruker D8 XRD)
Thermogravimetric Analysis
Attenuated Total Reflectance - Fourier Transform Infrared Spectroscopy (ATR-FTIR)
Pair Distribution Function Analysis (PDF) (Data generated at Argonne National Laboratory)

## Slide 7: Materials & Methods
Al/Si | 0.1 (NaAlO2)
Ca/Si | 0.6/1.2 (Ca(OH)2)
NaOH | 0.5/5M
4, 10-day | 1, 2, 3-month intervals

## Slide 8: Findings

## Slide 32: Conclusion
• C-S-H and Portlandite phases increase with higher alkalinities.
• the atom-atom distances decrease with alkalinity = denser morphology
• Silica interconnectivity increases within nanocrystalline structure.
• Highly alkaline samples contain less H2O
• Strong presence of unreacted silica fume in the matrix.
• Carbonation is extremely invasive.
• Atom-atom relations ≥8Å are nonexistent (amorphous gels).

## Slide 33: Further work
Carbonation prevention;
Use of additional techniques (e.g. 29Si-NMR spectroscopy)
XRD-PDF using more advanced instruments (Argonne Synchrotron)

## Slide 34: References
[1] Morten Daugaard Andersen, Hans J. Jakobsen, and Jørgen Skibsted. Incorporation of aluminum in the calcium silicate hydrate (c−s−h) of hydrated portland cements: a high-􀮹􀮭eld 27al and 29si mas nmr investigation. Inorganic Chemistry, 42(7): 2280–2287, 2003. doi: 10.1021/ic020607b. URL http://dx.doi.org/10.1021/ ic020607b. PMID: 12665361.
[2] David J. Belton, Olivier Deschaume, and Carole C. Perry. An overview of the fundamentals of the chemistry of silica with relevance to biosilici􀮹􀮭cation and technological advances. FEBS Journal, 279(10):1710–1720, 2012. ISSN 1742-4658. doi: 10.1111/j.1742-4658.2012.08531.x. URL http://dx.doi.org/10.1111/j.1742-4658. 2012.08531.x.
[3] Leon Black, Chris Breen, Jack Yarwood, Krassimir Garbev, Peter Stemmermann, and Biliana Gasharova. Structural features of c–s–h(i) and its carbonation in air—a raman spectroscopic study. part ii: Carbonated phases. Journal of the American Ceramic Society, 90(3):908–917, 2007. ISSN 1551-2916. doi: 10.1111/j.1551-2916.2006. 01429.x. URL http://dx.doi.org/10.1111/j.1551-2916.2006.01429.x.
[4] Je􀮸frey J. Chen, Je􀮸frey J. Thomas, Hal F.W. Taylor, and Hamlin M. Jennings. Solubility and structure of calcium silicate hydrate. Cement and Concrete Research, 34(9): 1499 – 1519, 2004. ISSN 0008-8846. doi: http://doi.org/10.1016/j.cemconres.2004. 04.034. URL http://www.sciencedirect.com/science/article/pii/ S000888460400211X. H. F. W. Taylor Commemorative Issue.
[5] J. Davidovits. Geopolymer chemistry and applications. Institue Geopolymere, Saint-Quentin, 2008.
.
.
.
For a complete list of citations please refer to: http://theonovak.com/files/projects/senior_thesis/theodosios_dimitrasopoulos_thesis_final.pdf

## Slide 35: Thank you
Claire White;
Nishant Garg; Eric McCaslin;
The Argonne National Laboratory;
The CEE Department;
My classmates;